**Fabrication and Characterization of Ni-Carbon nanofibers by Electrospinning Technique**

Pujashree Priyadarshini Sethy and Bibekananda Sundaray

Department of Physics, Ravenshaw University, Cuttack-753003, Odisha, India

E-mail: [pujashreepriyadarshini@gmail.com](mailto:pujashreepriyadarshini@gmail.com)

**Abstract:**

Carbon nanofibers with the distribution of magnetic Ni metal (Ni-CNFs) have been synthesized using Nickel (II) acetate tetrahydrate (Ni (OCHCH3)2.4H2O), polyacrylonitrile (PAN) as precursors by electrospinning technique. The as-prepared nanofibers were dried in a vacuum oven, stabilized, and followed by carbonization at 850 °C in N2 atmosphere. Their structural phase composition, microstructure, and magnetic properties have been studied. The X-ray diffraction (XRD) pattern confirms the formation of pure Ni-CNF phases without any impurity. The average diameter of the nanofibers and the Ni nanoparticles has been calculated to be 159±25.72 nm and 67±11.24 nm respectively. The presence of the elements Ni and C has been confirmed by energy-dispersive x-ray spectroscopy (EDX) measurement. Raman spectrum attributes the presence of two characteristic absorption peaks of carbon materials. Room temperature (300 K) magnetic measurement shows the ferromagnetic behavior of Ni-CNF. These nanofibers have the potential to be used as soft magnetic materials, magnetic sensors, and magnetic recording devices, etc.

**Keywords:** Ni-CNF,Electrospinning, XRD, Morphology, Ferromagnetic properties

**References:**

[1] N. A. M. Barakat, B. Kim and H. Y. Kim, Production of Smooth and Pure Nickel Metal Nanofibers by the Electrospinning Technique: Nanofibers Possess Splendid Magnetic Properties, J. Phys. Chem. C, *113,* 531–536, (2009), <https://doi.org/10.1021/jp805692r>.

[2] M. Adabi and M. Adabi, Electrodeposition of nickel on electrospun carbon nanofiber mat electrode for electrochemical sensing of glucose, J. Dispers. Sci. Technol, 42, 262-269, (2019), <https://doi.org/10.1080/01932691.2019.1678483>.

[3] Z. Bai, S. Liu, P. Chen, G. Cheng, G. Wu, H. Li and Y. Liu, Nickel nanoparticles embedded in porous carbon nanofibers and its electrochemical properties, Nanotechnology, 31, 30, (2020), <https://doi.org/10.1088/1361-6528/ab8594>.

[4] B. Ma, Y. Huang , C. Zhu , C. Chen, M. Fan, D. Sun, A facile method to synthesize carbon coated Fe, Co and Ni and an examination of their magnetic properties, J. Alloys Compd, 687, 741-745, (2016), <https://doi.org/10.1016/j.jallcom.2016.06.187>.